CrN

properties:
color --- silver
microhardness --- Hv1600 - 1800
coefficient of friction --- 0.3
thickness --- 1 - 40µm
thermal tolerance --- 700ºC
coating temperature --- 300ºC - 500ºC
adhesive force --- >60N
◎corrosion resistance
◎welding resistance
◎wear resistance
◎low friction
Application:
◎Dies for Mg, Cu, Zn, Ni, Al, alloy
◎molds for plastics
◎threading dies
◎parts of mobiles
◎mechanical parts

TiCN

properties:
color --- brown, purple, gray, black
microhardness --- Hv2800 - 3000
coefficient of friction --- 0.4
thickness --- 1 - 4µm
thermal tolerance --- 300ºC
coating temperture --- 300ºC - 500ºC
adhesive force --- >60N
◎wear resistance
◎welding resistance
◎corrosion resistance
Application:
◎cutting tools
◎punches and dies for cold working
◎plastic molds
◎mechanical parts
◎decorative parts

TiN

propertis :
color --- gold
microhardness --- Hv2000 - 2400
coefficient of friction --- 0.5
thickness --- 1 - 4µm
thermal tolerance --- 500ºC
coating temperature --- 300ºC - 500ºC
adhesive force --- >60N
◎wear resistance
◎welding resistance
◎corrosion resistance
appliction:
◎cutting tool
◎punches and dies for cold working
◎plastic molds
◎mechanical parts
◎decorative parts

TiX

properties:
color --- light parchment gold
microhardness --- Hv2300
coefficient of friction --- 0.3
thickness --- 1 - 4µm
thermal tolerance --- 800ºC
coating temperature --- 300ºC - 500ºC
adhesive force --- >60N
◎corrosion resistance
◎wear resistance
◎welding resistance
◎thermal resistance
◎low friction
Applictation:
◎cutting tools for high speed & dry cutting
◎warm working punches and dies for SUS alloy steel alloy
◎mechanical parts